Precipitation Kinetics, Microstructure, and Equilibrium State of A2 and B2 phases in Multicomponent Al2.75CoCrFeNi Alloy

M. Aizenshtein a,b,*, E. Strumza a, E. Brosh b, S. Hayun a

a) Department of Materials Engineering, Ben Gurion University of the Negev, Israel

b) NRCN-Negev, Israel

* Corresponding author: aizensht@post.bgu.ac.il

Abstract

AlxCoCrFeNi high-entropy alloys have received significant attention recently because of their promising mechanical and corrosion-resistance properties. These alloys tend to form a mixture of fcc and bcc phases, where the latter has an important role in material hardening. In many cases, the bcc phase is a mixture of disordered bcc (A2), which is an Fe- and Cr-rich phase, and ordered bcc (primitive cubic, B2), which is an Al-, Ni-, and Co-rich phase. Although phase diagrams above x = 2 are somewhat consistent, they unfortunately contain no valuable data about the mole fraction and phase composition.

Moreover, Alx>2CoCrFeNi alloys suffer from a lack of systematic experimental investigation into the kinetics of the phase transformation. To clarify these points, the present study investigates the phase relations and precipitation kinetics of A2 from the B2 matrix in Al2.75CoCrFeNi. The results show that the compositions of the A2 and B2 phases are temperature dependent and that, with increasing temperature in the B2 phase, the Al content decreases while the Cr content increases, which correlates with thermodynamic calculations. In addition, the equilibrium composition and phase content lead to a reduced lattice distortion parameter compared with that of the nominal alloy.

Concerning the kinetics of phase transformation, the results suggest that, to precipitate in the solid state, the A2 phase within the B2 matrix must overcome the internal stress that is due to the different lattice parameters of the two phases. Furthermore, the diffusion activation energy is estimated and its implications discussed from the perspective of sluggish diffusion in multicomponent systems. Finally, the coefficients of thermal expansion of Al2.75CoCrFeNi alloy and of Al-Ni-Co-and Cr-Fe-rich alloys (both alloys containing Al, Co, Cr, Fe, Ni) were measured and are discussed in relation to phase transformation.

Keywords: Al2.75CoCrFeNi, Microstructure, Thermodynamics, Lattice Distortion Parameter

Introduction

High-entropy alloys (HEAs), and specifically the Al0<x<2CoCrFeNi system, have received significant attention due to their promising mechanical and corrosion-resistance properties [1–5]. The Alx(0.1<x<1.2)CoCrFeNi series contains a mixture of simple structures, such as fcc and bcc, of which the bcc phase plays a vital role in hardening the alloy [6]. The volume fraction of the bcc phase increases with increasing Al content.

In many cases, the bcc phase is a mixture of a disordered bcc phase that is relatively rich in Fe and Cr (called the “A2” phase) and an ordered bcc phase that is richer in Al-Ni-Co (primitive cubic, called the “B2” phase) [7]. Nevertheless, published phase diagrams [8,9] give incomplete information about the equilibrium fraction of each phase, the temperature dependence of the phase composition, and the precise temperature of the phase transition. Interestingly, for AlxCoCrFeNi systems, in composition ranges where both the A2 and B2 phases exist, the volume fraction of the ordered B2 phase increases with temperature whereas the volume fraction of the disordered A2 phase decreases and eventually disappears.

In AlCoCrFeNi-based HEAs, Al reportedly stabilizes both the disordered A2 and ordered B2 structure [8], provided the latter is favored, and Cr stabilizes the A2 structure and destabilizes both B2 and fcc structures [10,11]. Thus, in the present work, we study mixed A2 and B2 phases in the Al2.75CoCrFeNi alloy by both measuring and calculating the composition of the two phases at equilibrium. The results and discussion first treat the equilibrium state, assuming that A2 and B2 phases reach compositional equilibrium after prolonged heat treatment. The experimental results are then compared with thermodynamic calculations.

We also calculate and discuss the lattice distortion parameter , which is unique to multicomponent systems, in relation to the compositional changes at equilibrium.

The second part discusses the kinetics of the precipitation of the A2 phase from the B2 matrix, including the estimates of the diffusion activation energy and the role played by stress induced between the two phases. The coefficients of thermal expansion (CTEs) of the Al2.75CoCrFeNi alloy and of the Al-Ni-Co- and Cr-Fe-rich alloys (both containing Al, Co, Cr, Fe, Ni) were measured, revealing a significant difference between the CTE of the A2 and B2 phases, which is discussed in the view of phase-transformation kinetics.

Experiment

Sample preparation and heat treatments

Three alloys with different nominal compositions (Table 1) were prepared by a nonconsumable electrode arc melting in an ultrahigh-purity argon atmosphere using a Ti getter. To answer specific questions about the properties of the A2 and B2 phases, the composition of the latter two alloys was chosen based on the characterization of the Al2.75CoCrFeNi alloy. The raw materials with purities greater than 99.9% were melted and turned over five times for improved homogeneity, followed by a final stage of arc-melting using a 6-mm-diameter rod. For heat-treatment experiments, the “as-cast” Al2.75CoCrFeNi samples were cut from the cast rod, wrapped in tantalum foil, and sealed in quartz capsules. The samples then were heat treated at various temperatures and for various durations, as detailed in Table 2. Following heat treatment, the samples were either water quenched or furnace cooled.

Table 1. Nominal compositions.

| Alloy | Al [at%] | Co [at%] | Cr [at%] | Fe [at%] | Ni [at%] |
| --- | --- | --- | --- | --- | --- |
| Al2.75CoCrFeNi | 40.80 | 14.80 | 14.80 | 14.80 | 14.80 |
| Al-Ni-Co rich | 38 | 20 | 6 | 12 | 24 |
| Cr-Fe rich | 22 | 7.00 | 43 | 25 | 5 |

To assess the heat-treatment conditions, the heat-treatment duration was approximated by using the diffusion coefficients of Ni published for a similar system [12] and a typical diffusion length of about 1 m (typical dimension of the “coarsening volume”) based on transmission electron microscopy (TEM) characterization of the as-cast sample. To coarsen the microstructure, the dwell time t is estimated by using r2Dr2D, where r is the diffusion length and D is the diffusion coefficient. In this case, the estimated dwell time at 800, 900, 1000, 1100, 1200, and 1300 °C is 279 h, 15 h, 1.5 h, 10 min, 1.6 min, and 20 s, respectively. Much longer heat treatments were used in practice to ensure sufficiently coarse phases.

Table 2 Heat-treatment parameters of the Al2.75CoCrFeNi samples. All samples were water quench unless otherwise mentioned.

| Temperature [°C] | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1300* |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Time [hours] | 264 | 164 | 139 | 98 | 65 | 4 | 4 |

* Furnace cooling.

Characterization

X-ray powder diffraction (XRD) was done by using an Empyrean Alpha 1 diffractometer (Malvern Panalytical Ltd, Royston, UK) with Cu Kα radiation. The operating parameters were 40 kV and 30 mA and the 2θ range spanned from 20° to 120° with a step size of 0.02° and a scan step time of 1 s. Lattice parameters and phase composition were refined from the diffraction patterns by using a whole-pattern-fitting approach implemented in the MDI Jade 2010 software package (version 2.8.1, 2014, Materials Data, Livermore, CA, USA).

Prior to measurements, the sample was ground to fine powder by using a mortar and pestle. Microstructure and compositional analysis were done by scanning electron microscopy (Extremely-High-Resolution SEM, Verios XHR 460L, OR, USA) equipped with a Noran energy dispersive spectrometer (EDS) operated at 15 keV. Samples for SEM characterization were prepared by following a standard procedure that included a final stage of polishing with 1 µm diamond paste. TEM (JEOL JEM-2100F, Peabody, MA, USA) was used to image selected samples. TEM samples were extracted from SEM samples by using a focused ion beam (Helios G4 UC, Thermo-Fisher Scientific, MA, USA). Bright- and dark-field TEM (BF and DF-TEM) were used to characterize the sample morphology. Finally, selected area electron diffraction was used to characterize the structural phases of the material.

Thermal expansion

Thermal expansion experiments were done from room temperature to 1350 °C by using a dilatometer (L75 horizontal dilatometer Linseis, Selb, Germany) operating in continuous mode with an α-Al2O3 push rod. The temperature was monitored by using an S-type thermocouple. The temperature was calibrated during heating by melting Sn, Ag, and Au standards in alumina crucibles. Measurements were made in an ultrahigh-purity Ar (99.999%) atmosphere using continuous heating at 3 °C/min. Instrumental effects were accounted for by running an Al2O3 reference sample using ASTM E228-17.

Thermodynamic analysis

The thermodynamic analysis used the database developed by Hallstedt [13] and the Thermo-Calc software [14]. The calculation takes into account four sublattices for the fcc phase, A2 and B2 bcc phases, and phase.

Results and Discussion

Microstructure and composition and equilibrium state

Figure 1a presents a typical microstructure of an as-cast sample, the BSE analysis of which reveals a homogeneous dendrite structure with a typical length of 25–50 m. The XRD analysis was unable to clearly determine whether the A2 phase exists because it could overlap with the B2 phase (see Figure 1b).

(b)

(a)

100 m

(b)

(a)

100 m

Figure 1. As-cast Al2.75CoCrFeNi alloy: (a) SEM BSE image of polished sample etched for 20 s in aqua regia solution; (b) XRD pattern of powder sample showing the overlap of reflections from the A2 and B2 phases due to the similar lattice parameters of the two phases.

To clarify these results, the same sample was characterized in depth by using STEM and EDS x-ray mapping (Figure 2). The results indeed reveal two phases on the nanoscale: an Fe-Cr-rich phase with cubic morphology, and a second phase consisting of an Al-Ni-Co-rich matrix.

Based on data from Refs. [6,15], which also studied the microstructure and phase composition of Al0.9CoCrFeNi, Al1.5CoCrFeNi, and AlCoCrFeNi alloys, we conclude that the first phase is the disordered bcc (A2) phase, and the second phase is the ordered bcc (B2) phase. Thus, in the as-cast alloy, the A2 nanoparticles with cubic morphology are incorporated into the B2 matrix. The fine cubic microstructure and the significant number of A2 precipitates per unit area suggest that spinodal decomposition occurs during solidification. This finding is consistent with the results of Kao et al. [7] and Lv et al. [16]. Kao et al. [7] claim that the wall-shaped microstructure evolves after heat treatment at 1100 °C for 24 h in the Al0.875<x<2CoCrFeNi system as a result of spinodal decomposition. Lv et al. [16] also report that spinodal decomposition occurs in Alx=0.5,0.75,1CoCrFeNi alloys prepared by arc-melting and suction casting.

(d)

(d)

(c)

(c)

(b)

(b)

(f)

(f)

(e)

(e)

(a)

(a)

Figure 2. X-ray mapping of (a) Al, (b) Co, (c) Ni, (d) Cr, and (e) Fe elements and (f) a dark-field image from as-cast Al2.75CoCrFeNi using TEM (EDS).

Figure 3 shows the evolution of the A2 morphology as a function of temperature. The cubic-like A2 morphology (bright phase) detected by STEM analysis (Figure 2) becomes more coarse and maintains its cubic morphology up to 800 °C. At 900 °C, the A2 phase loses its cubic-like morphology and the phase islands become rounder.

(b)

2 m

(a)

1 m

(c)

2 m

2 m

(d)

5 m

(d)

A2

B2 matrix

A2 precipitates

B2 matrix

B2 matrix

A2 precipitates

(b)

2 m

(a)

1 m

(c)

2 m

2 m

(d)

5 m

(d)

A2

B2 matrix

A2 precipitates

B2 matrix

B2 matrix

A2 precipitates

A2

A2

B2 matrix

B2 matrix

Figure 3 High-resolution-SEM BSE images of the equiaxed A2 precipitates in Al2.75CoCrFeNi at (a) 800 °C, (b) 900 °C, (c) 1000 °C, (d) 1100 °C, and (e) 1200 °C. Bright gray phase or particles is the A2 phase, darker gray matrix is the B2 phase. Examples of A2 precipitates are circled.

Above 900 °C, two types of A2 morphologies are identified (Figure 4). The first A2 morphology consists of threads that decorate the grain boundaries, whereas the second A2 morphology is rounder, more equiaxed, and is located mainly in the bulk of the grains. Both A2 morphologies have the same elemental composition. With increasing temperature and time, both morphologies become coarser; the bulk-grain A2 phase maintains its rounded shape, and the grain-boundary A2 phase becomes thicker (Figure 4). Because the diffusion coefficient at grain boundaries is orders of magnitude greater than that in the bulk, we focus on the inter-grain A2 precipitates.

20 m

A2 precipitates

20 m

A2 precipitates

Figure 4 BSE image of the Al2.75CoCrFeNi alloy after heat treatment at 1200 °C for 50 h followed by a direct treatment at 1000 °C for 25 h shows an example of sub-grain A2 phase (bright areas are A2 phase, darker areas are B2 matrix). Examples of A2 precipitates are encircled.

The composition and volume fractions of A2 and B2 phases as a function of temperature and time were also studied, Table 3 and Figures 5 and 6 summarize the results together with calculated values based on a thermodynamic analysis using the Thermo-Calc software and the new thermodynamic database for HEAs developed by Hallstedt [13].

Figure 5 (a) Al and (b) Cr content in the B2 phase of Al2.75CoCrFeNi alloy as a function of temperature. Experimental results are compared with thermodynamic calculations.

Figure 6 A2, B2, and liquid molar fraction in the Al2.75CoCrFeNi alloy as a function of temperature based on a thermodynamic analysis using the Thermo-Calc software and the new thermodynamic database for HEAs developed by Hallstedt [13].

Table 3 Measured and calculated composition of A2 and B2 phases in heat-treated Al2.75CoCrFeNi samples. A2 and B2 mole fractions were obtained from a thermodynamic calculation and volume fractions were obtained from EDS analysis (mole fraction ≈ volume fraction).

| Phase | Temperature [°C] | Al | Co | Cr | Fe | Ni | Vol. fraction |
| --- | --- | --- | --- | --- | --- | --- | --- |
| B2 | 900 | 46.8±0.8 | 17.3±0.2 | 5.5±1.0 | 12.4±0.2 | 18.0±0.2 | 0.68±0.03 |
|  | 1000 | 45.1±0.5 | 17.5±0.4 | 6.4±0.7 | 12.4±0.4 | 18.6±0.4 | 0.76±0.01 |
|  | 1100 | 43.4±0.4 | 17.6±0.5 | 7.6±0.2 | 13.2±0.2 | 18.2±0.6 | 0.81±0.02 |
|  | 1200 | 42.2±0.2 | 17.2±0.5 | 8.8±0.3 | 14.0±0.3 | 17.8±0.2 | 0.84±0.03 |
| B2- Thermo-Calc | 900 | 45.75 | 17.48 | 3.25 | 15.84 | 17.68 | 0.84 |
|  | 1000 | 45.03 | 17.12 | 4.91 | 15.44 | 17.50 | 0.85 |
|  | 1100 | 44.13 | 16.58 | 7.03 | 15.14 | 17.13 | 0.86 |
|  | 1200 | 43.02 | 15.92 | 9.58 | 14.94 | 16.53 | 0.89 |
| A2 | 900 | 30.9±1.0 | 8.5±0.6 | 34.2±0.7 | 19.8±0.5 | 6.6±0.6 | 0.32±0.03 |
|  | 1000 | 22.7±0.5 | 5.7±0.8 | 44.5±0.5 | 23.6±0.7 | 3.5±0.6 | 0.24±0.01 |
|  | 1100 | 16.6±0.5 | 6.9±0.4 | 46.3±0.2 | 27.5±0.3 | 2.7±0.1 | 0.19±0.02 |
|  | 1200 | 21.5±0.1 | 5.3±0.3 | 47.8±0.2 | 23.0±0.3 | 2.4±0.4 | 0.16±0.03 |
| A2- Thermo-Calc | 900 | 14.96 | 1.08 | 74.36 | 9.55 | 0.05 | 0.16 |
|  | 1000 | 17.24 | 2.21 | 69.02 | 11.38 | 0.14 | 0.15 |
|  | 1100 | 19.63 | 3.83 | 63.35 | 12.81 | 0.37 | 0.14 |
|  | 1200 | 22.15 | 5.79 | 57.42 | 13.82 | 0.82 | 0.11 |
| Alloy composition | 900 | 40.9±1.0 | 14.6±0.4 | 15.0±1.0 | 14.7±1.6 | 14.8±0.8 |  |
|  | 1000 | 40.1±1.0 | 14.7±0.3 | 15.2±0.1 | 15.3±0.6 | 14.7±0.4 |  |
|  | 1100 | 38.1±1.0 | 15.6±0.8 | 15.6±0.2 | 15.5±0.7 | 15.2±1.0 |  |
|  | 1200 | 38.8±1.0 | 15.5±0.2 | 14.9±1.0 | 15.6±1.0 | 15.2±0.6 |  |

Table 3 compares the measured Al and Cr content in the B2 phase as a function of temperature with the calculated composition (see also Figure 5). The thermodynamic calculations are consistent with the experimental results: the concentration of the Al decreases with rising temperature whereas that of Cr increases with rising temperature. This result affects the lattice distortion parameter, which is a fundamental parameter in HEAs and is discussed further below.

Lattice distortion

The data given in Table 3 reveal that, with increasing temperature, the Al and Cr content in the B2 phase decreases and increases, respectively. This section shows how these results affect the lattice-distortion parameter. Previous studies [16, 17] that aimed to find a single property to characterize the multi-component solid-solution systems suggest using the atomic-size difference , which is defined as

δ=i=1nci1-riri2  ,       (2)

where ci is the atomic fraction of component i, ri is the atomic radius (143, 125, 129, 126, and 125 pm for Al, Co, Cr, Fe, and Ni, respectively [18]) andri ri= i=1nciri is the average atomic radiusri= i=1nciri.

The atomic-size difference  is proportional to the lattice distortion, so a large implies a large lattice distortion. Figure 7 shows  as a function of Al composition in AlxCoCrFeNi. The calculation considers that the stoichiometries of four elements remain constant, and one element changes its stoichiometry. For example, when Al changes its stoichiometry from 1 to 4.5, all other elements remain at unity stoichiometry. As other elements (e.g., Fe, Co, Cr, or Ni) change stoichiometry from 1 to 1.5, all remaining elements maintain constant at unity stoichiometry (e.g., Al = 2.75, and Fe, Co, Cr, and Ni =1). As the Al content increases,  increases up to a stoichiometry of 3.5 (~47 at.%) and then decreases slightly. Ni and Co have the same effect on  because they have the same atomic radii, so they cause  to increase, but much less so than Al. Adding Cr and/or Fe decreases , but Cr is much more dominant. These observations qualitatively explain the increase in Cr and Fe in the precipitated A2 phase. Table 4 summarizes  calculated based on the composition of A2 and B2 and their volume fractions from Table 3. The results indicate that the atomic-size difference  of the A2 phase is less than that of the B2 phase. Thus, the precipitation of A2 from the B2 matrix will reduce compared with its nominal value, which may suggest that, despite the stabilization of B2 by the significant Al content, it remains insufficient to overcome the larger distortion in the B2 structure, so a mixture of the A2 and B2 phases still exist up to 1270 °C (as per Figure 6).

Figure 7 Lattice distortion as a function of stoichiometry of the various elements according to Eq. (1).

Table 4 nominal for Al2.75CoCrFeNi = 0.0626.

|  | 900 °C | 1000 °C | 1100 °C | 1200 °C |
| --- | --- | --- | --- | --- |
| A2 | 0.0561 | 0.0491 | 0.0457 | 0.0491 |
| B2 | 0.0651 | 0.0647 | 0.0645 | 0.0641 |
|  weighted average* | 0.0623 | 0.0613 | 0.0619 | 0.0623 |

*       δA2*XA2+ δB2*XB2=δweighted average where X is the volume fraction of the phase.

Kinetics and nonequilibrium state

Effect of cooling rate on microstructure

The morphology of A2 depends not only on the heat-treatment temperature but also on the cooling rate. Figure 8 shows the microstructure of two samples after heat treatment at 1300 °C for 4 h: one sample was water quenched and the other was furnace cooled to room temperature. In the case of slow cooling (i.e., furnace cooling), two morphologies of the A2 phase appear: one at the subgrain boundaries and one within the bulk of the subgrains. The subgrain boundaries are decorated by a continuous A2 phase whereas, in the vicinity, the area is almost A2 free. Within the subgrains, the A2 phase presents a submicron needle-like morphology. In the case of rapid cooling (i.e., the water-quenched sample), the BSE image shows a rather uniform composition whereas the grain boundaries (~200–300 m) are brighter, which means that their average atomic number is higher than that of the bulk regions of the grains. TEM imaging of the quenched sample reveals the presence of spherical nanoparticles within the B2 matrix (Figure 8d). These results show that standard quenching does not conserve a solo B2 phase structure as predicted by the thermodynamic analysis. This finding may be due to the large lattice distortion of the B2 phase. Furthermore, the density of the A2 precipitates implies that no or few nucleation barriers hinder its formation.

A2 precipitates

A2 precipitates

(c)

(c)

201

100 nm

201

100 nm

10 m

(a)

(b)

2 m

(d)

300 m

10 m

(a)

(b)

2 m

(d)

300 m

(c)

(c)

Figure 8 Al2.75CoCrFeNi heat treated to 1300 °C samples (a), (b) High-resolution-SEM BSE image, furnace cooled (i.e., slow cooling); (c) BSE image of water-quenched sample (i.e., rapid cooling); (d) TEM dark-field image of water-quenched sample. The circled reflection (201) is forbidden for the A2 structure. In panel (b), examples of A2 precipitates (light gray) are circled.

Precipitation kinetics

Because the precipitate growth is diffusion controlled, we applied the Lifshitz and Slyozov theorem [19] concerning the kinetics of precipitation from supersaturated solid solution. According to Lifshitz and Slyozov [19], the average radius R3=α*Dt of the precipitates, where α* contains geometrical constants and weakly-temperature-dependent coefficients in the solid state such as surface tension, D is the diffusion coefficient, and t is time. If α* is considered constant, then α*D=D*, where D* obeys the same Arrhenius relation as D:

D(T)=cConst×∙exp⁡(-Q/RT),   (1)

where Q Jmol is the activation energy, RJmol∙K is the universal gas constant, and T K is the absolute temperature.

By using the measured average diameter of A2 precipitates as a function of temperature (Table 5), the activation energy Q was extracted from the slope of lnD vs 1/T (Figure 9). The calculated activation energy for A2 precipitation in Al2.75CoCrFeNi is thus 323 ± 39 kJ/mol. The result is within the margin of error of other published data on multicomponent systems, but on the high side. For example, Nadutov et al. [20] report an activation energy of 306.9 kJ/mol for the precipitation of a bcc phase from a mixture of fcc and bcc phases in Al(х=1,1.5,1.8) FeNiCoCuCr, and Vaidya et al. [12] report an activation energy of 303.9 ± 8.7 kJ/mol for diffusion in the CoCrFeMnNi fcc phase.

Table 5 Average diameter of A2 precipitates after various heat treatments.

| Temperature [°C] | Average diameter d [nm] | t [hr] |
| --- | --- | --- |
| 800 | 93±28 | 264 |
| 900 | 450±129 | 164 |
| 1000 | 560±162 | 139 |
| 1100 | 1216±462 | 98 |
| 1200 | 1849±564 | 65 |

Figure 9 ln(D) as a function of 1/T, where D is the diffusion coefficient and T is the absolute temperature.

A qualitative explanation for the higher activation energy obtained in the present work may be related to the lattice distortion in multicomponent systems. First, in multicomponent systems, the diffusion rate generally decreases with increasing number of components [21] (this is due to a high activation energy or a low pre-exponential coefficient). However, the calculation of the lattice-distortion parameter for AlхFeNiCoCuCr (Nadutov et al. [20], for Al = 1.8) gives δ = 0.0563 (the atomic radius for Cu is 128 pm), which is less than the nominal value for the alloy Al2.75CoCrFeNi (Table 4). For the alloy CoCrFeMnNi (Vaidya et al.[12]), the atomic radius of Mn (137 pm) is less than that of Al and the Mn content in the alloy is also less than that of Al in Al2.75CoCrFeNi, so the distortion parameter is δ = 0.0354, which is significantly less than the value of  for the Al2.75CoCrFeNi alloy.

Beke and Erdelyi [11] claim that the sluggish diffusion is characteristic of HEAs (multicomponent systems where the content of each component is 5–35 at.%). Compared with pure metals, this result is attributed primarily to the temperature-independent factor in the diffusion coefficient rather than to the higher activation energies. As argued below, this statement also applies to the alloy Al2.75CoCrFeNi; moreover, the role of lattice distortion is demonstrated.

If we assume similarities between multicomponent systems and use the data of Nadutov et al. [20] for the diffusion coefficient, the diffusion coefficient for the Al2.75CoCrFeNi system at 1200 °C would be about  5×∙10-15 m2sm2sec. When compared with the self-diffusion of vanadium (as done in Ref. [11]), which is also a bcc structure, at the same homological temperature (TTmeltingTTmelting=0.88) D=1.84×∙10-11 m2sm2sec, despite its high activation energy (394 kJ/mole). Actually, the diffusion coefficient should be compared with the AlNi intermetallic (B2 phase with a lattice parameter of 0.288 nm [22]) because the B2 phase in this study is an ordered Al-Ni phase. The activation energy for AlNi is 307 kJ/mole, and the diffusion coefficient at the homological temperature of 0.88 is 1.3×∙10-13 m2sm2sec, which is again almost two orders of magnitude greater than for the multicomponent system.

In the diffusion expression, consider now the pre-exponential factor D0, which is proportional to a2υ, with a being the lattice constant and υ the Debye frequency. The calculated average weighted lattice parameter of Al2.75CoCrFeNi is 0.340 nm compared with 0.287 nm of the bcc phase (this result by itself implies the existence of lattice distortion), which means a reduction of about 30% in D.

Li et al. [23] correlated the increase of Al content in AlxCoCrFeNi with the increase in lattice distortion and alloy hardness and obtained a hardness ratio for xAl=1 to xAl=2.75 of Hx=1Hx=2.75Hx=1Hx=2.75=0.66. As seen in Figure 7, a decrease in Al content from 2.75 to 1 reduces  by 15%. As for the average weighted lattice parameter for xAl=1 (0.317 nm), given the lattice parameter of the B2 phase [23], D is reduced only by 10%, which equates to a greater diffusivity for lower Al content (and lower lattice distortion) in the alloy AlxCoCrFeNi.

Volume changes due to B2-to-A2 phase transformation

First-order phase transformations in solids are usually accompanied by volumetric changes. The sign of this change (i.e., expansion or contraction) could affect the transformation kinetics. To clarify this point, we extracted the lattice parameter of each phase from the room-temperature XRD pattern, measured the CTE of the alloy Al2.75CoCrFeNi, and attempted to synthesize the single phase to determine the CTE of each phase.

XRD analysis

Figure 10 shows a representative XRD pattern from the heat-treated samples, clearly revealing both the A2 and B2 phases. In general, the B2 phase has smaller lattice parameters than the A2 phase. For example, in the sample heated to 1200 °C for 65 h and then rapidly quenched, aB2 = 0.2882(1) nm and aA2= 0.2898(1) nm. The B2 lattice parameter is thus smaller by 0.4% to 0.5% with respect to the A2 lattice parameter. Note that the equilibrium lattice parameters reported herein differ from those reported in the literature; for example, Tang et al. [24] report that the A2 and B2 phases in the alloy AlCoCrFeNi have the same lattice parameter of a = 0.287 nm. This difference may be due to the high Al content in the alloy AlxCoCrFeNi, similar to the results of Nair et al. [25], who reported that aA2 for the alloy Al3CoCrFeNi is significantly greater than aB2 (0.294 versus 0.287 nm). In addition, Wang et al. [6] and Li et al. [23] reported that that the lattice parameter of the bcc phases increases with increasing Al content in Alx(1≤x≤3)CoCrFeNi. Thus, although the lattice parameters are the same at x = 1, as the Al content in the alloy increases, the lattice parameter of the A2 phase increases faster than that of the B2 phase, as observed at x = 2.75.

Figure 10 XRD pattern of Al2.75CoCrFeNi sample, heat treated at 1200 °C for 65 h and rapidly quenched: (a) overall plot, (b) whole-pattern fitting showing the calculated pattern for A2 (red line), B2 (green line), and their sum (black line), which matches the experimental pattern shown below.

To clarify this deviation from the published results and also to measure the CTE of each phase, two alloys with a composition similar to that of the B2 (Al-Ni-Co-rich) and A2 (Cr-Fe-rich) phases were prepared (Table 1). The compositions of each phase were chosen according to the data given in Table 3 and were close to the composition of the B2 phase reported by Tang et al. [24] and Yang et al. [26]. XRD (Figure 11) and TEM analyses show that the Al-Ni-Co-rich alloy is a single B2 phase, whereas the Cr-Fe-rich alloy contains a small amount of B2 (Figure 11). The lattice parameter of the Al-Ni-Co-rich alloy is 0.2879(1) nm, which differs by about 0.01% from the lattice parameter of the B2 phase in Al2.75CoCrFeNi. The lattice parameter of the Cr-Fe-rich alloy is 0.2890(1) nm, which differs by about 0.03% from the lattice parameter of the A2 phase in Al2.75CoCrFeNi. These results confirm that, for Al2.75CoCrFeNi, the lattice parameter of the A2 phase is larger than the lattice parameter of the B2 phase by about 0.4%, which means that, to precipitate in the solid state, the A2 phase must overcome internal stress at the A2-B2 interface.

Figure 11 XRD pattern of the Al-Ni-Co rich and Cr-Fe rich alloys.

Thermal expansion

Figure 12 shows the CTEs for the B2 (Al-Ni-Co-rich) and A2 (Fe-Cr-rich) phases and the alloy Al2.75CoCrFeNi. The A2 phase and Al2.75CoCrFeNi have the same CTEs between 300 and 1350 °C and the CTE-vs-temperature slope changes at 1256 °C because the sample shrinks. Conversely, the B2 phase has the same CTE as the A2 phase and Al2.75CoCrFeNi up to 450 °C but, at higher temperatures, the B2 phase has a smaller CTE, and the CTE-vs-temperature slope changes at 1033 °C because of shrinkage. Chou et al. [27] studied the thermophysical and electrical properties of AlxCoCrFeNi (0 ≤ x ≤ 2) HEAs and reported that the AlxCoCrFeNi alloys are ferromagnetic and that additional expansion occurs due to magnetic ordering. They also reported that the CTE in the bcc phase of Alx(1.25≤x≤2)CoCrFeNi decreases from 13.35 ×10−6 K−1 to 12.85 ×10−6 K−1 from 423 to 773 K, which is reasonably consistent with the present results. These differences would add a significant amount of about 0.6% to the stresses between the A2 and B2 phases and will contribute to the suppression of the B2-to-A2 phase transformation upon cooling the alloy. For the A2-to-B2 phase transformation, this contraction stress promotes the phase transformation.

Figure 12 CTE as a function of temperature for the Al2.75CoCrFeNi alloy, the B2 phase (i.e., Al-Ni-Co-rich alloy), and the A2 phase (i.e., Fe-Cr-rich alloy).

The measured lattice parameters of the B2 and A2 phases show that the B2-to-A2 phase transformation involves a volume expansion, which imposes compressive stresses on the A2 phase. The CTE of the B2 phase is significantly smaller than that of the A2 phase. According to the whole-pattern fitting of the XRD data from the as-cast sample, the initial fraction of the A2 phase in the Al2.75CoCrFeNi alloy is about 22 vol.%. The data in Table 3 show that, at the lower temperatures of 800 and 900 °C, during the isothermal heat treatment, the volume fraction of the A2 phase increases, whereas in the higher temperature range of 1000–1200 °C, the fraction of the A2 phase decreases. In the first scenario, the B2 phase is surrounded by the A2 phase and is under tensile stress, which facilitates the B2-to-A2 phase transformation. In the second scenario, the A2 phase must transform into the B2 phase to reach equilibrium. Since the A2 phase is under compressive stress, the phase transformation should be retarded, but since the sample is above the homological temperature of 0.78, we assume that this stress is easily relieved and the transformation occurs more rapidly. In summary, the stress involved in the phase transformation studied herein does not seem to retard the phase transformation during isothermal heat treatments. However, should the A2 phase precipitate from a supersaturated solid B2 solution, the difference in lattice parameters between the two phases would increase with temperature, which would cause compressive stress on the A2 phase. The impact of this stress on the phase-transformation kinetics should not be ignored.

Summary and Conclusions

Limited studies have focused heretofore on AlxCoCrFeNi alloys with x >1.8 because of the high brittleness and lack of applicability of these alloys. Nevertheless, these alloys are scientifically interesting because they contain a mixture of ordered (B2) and disordered (A2) phases that exist with lower Al content in the form of potentially applicable AlxCoCrFeNi alloys.

The present study investigates the structure, composition, precipitation kinetics, and CTE of the Al2.75CoCrFeNi alloy and its phases. The experimental results are consistent with the published results and with thermodynamic calculations, in which this alloy contains only two phases: the ordered bcc (B2) phase and the disordered bcc (A2) phase. It is also confirmed both experimentally and thermodynamically that the composition of both phases is temperature dependent. For the B2 phase, upon increasing the temperature, the Al content decreases and the Cr content increases. This compositional change leads to a smaller distortion parameter. Moreover, the lattice parameter of the A2 phase is larger than that of the B2 phase; a finding that is well explained by invoking the increasing content of Al in the AlxCoCrFeNi alloy, which is consistent with the results of previous studies.

This investigation of the B2-only alloy and of a B2 alloy containing a significant fraction of A2 alloy allows us to distinguish between the properties of the two alloys. The CTE of the A2 phase is greater than that of the B2 phase. Interestingly, the CTE of Al2.75CoCrFeNi is similar to the CTE of the A2 phase. This result can be explained if we assume that, while heating the B2 supersaturated alloy, the B2 phase is under compressive stress, which may facilitate the sluggish B2-to-A2 phase transformation. Thus, any differences (i.e., lattice parameters and CTEs) between the A2 and B2 phases could affect the phase-transformation kinetics when both phases are involved. In fact, the precipitation kinetics in Al2.75CoCrFeNi and the estimated diffusion activation energy Q = 323 ± 39 kJ/mol support our assumption and are in a range similar to that of other multicomponent systems and AlNi intermetallic materials.

Acknowledgments

The authors would like to thank Dr. Bengt Hallstedt for permission to use his new thermodynamic database for HEAs. Gratitude also goes to Mr. Eyal Attal and Mr. Omri Azulai from the Physics Department at NRC-Negev, Israel, for their valuable technical assistance.

The authors declare that they have no conflict of interest.

References

[1] Chen Y.Y., Duval T., Hung U.D., Yeh J.W., and Shih H.C. (2005) Microstructure and electrochemical properties of high entropy alloys—a comparison with type-304 stainless steel. Corros. Sci. 47(9):2257–2279.

[2] Tsai C.W., Tsai M.H., Yeh J.W., and Yang C.C. (2010) Effect of temperature on mechanical properties of Al0.5CoCrCuFeNi wrought alloy. J. Alloys Compd. 490(1-2):160–165.

[3] Tong C.J., Chen M.R., Chen S.K., Yeh J.W., Shun T.T., Lin S.J., and Chang S.Y. (2005) Mechanical performance of the AlxCoCrCuFeNi high-entropy alloy system with multiprincipal elements. Metall. and Mat. Trans. A 36(5):1263–1271.

[4] Lu Y.P., Dong Y., Guo S., Jiang L., Kang H.J., Wang T.M., Wen B., Wang Z.J., Jie J.C., Cao Z.Q., Ruan H.H., and Li T.J. (2014) A promising new class of high-temperature alloys: eutectic high-entropy alloys. Sci. Rep. 4:6200.

[5] Munitz A., Salhov S., Hayun S., and Frage N. (2016) Heat treatment impacts the micro-structure and mechanical properties of AlCoCrFeNi high entropy alloy. J. Alloys Compd. 683:221–230.

[6] Wang W.R., Wang W.L., Wang S.C., Tsai Y.C., Lai C.H., and Yeh J.W. (2012) Effects of Al addition on the microstructure and mechanical property of AlxCoCrFeNi high-entropy alloys. Intermetallics 26:44–51.

[7] Kao Y.F., Chen T.J., Chen S.K., and Yeh J.W. (2009) Microstructure and mechanical property of as-cast, -homogenized, and -deformed AlxCoCrFeNi (0 ≤ x ≤ 2) high-entropy alloys. J Alloy Compd. 488(1):57–64.

[8] Zhang C., Zhang F., Chen S., and Cao W. (2012) Computational dynamics aided high-entropy alloy design. JOM 64(7):839–845.

[9] Zhang C. and Gao M.C. (2016) CALPHAD Modeling of High-Entropy Alloys. in Gao M.C., Yeh J.W., Liaw P.K., and Zhang Y. (eds) High-Entropy Alloys Fundamentals and Applications. Springer, Switzerland, p. 422.

[10] Tsai K.Y., Tsai M.H., and Yeh J.W. (2013) Sluggish diffusion in Co–Cr–Fe–Mn–Ni high-entropy alloys Acta Mater 61(13):4887–4897

[11] Beke D.L. and Erdelyi G. (2016) On the diffusion in high-entropy alloys. Mater. Lett. 164:111–113.

[12] Vaidya M., Trubel S., Murty B.S., Wilde G., and Divinski S.V. (2016) Ni tracer diffusion in CoCrFeNi and CoCrFeMnNi high entropy alloys. J. Alloys Compd. 688:994–1001.

[13] Hallstedt B. (2017), private communication.

[14] Andersson J.O., Helander T., Hoglund L., Shi P.F. and Sundman B. (2002) Thermo-Calc and DICTRA, Computational tools for materials science. Calphad 26(2):273–312.

[15] Linden Y., Pinkas M., Munitz A., and Meshi L. (2017) Long-period antiphase domains and short-range order in a B2 matrix of the AlCoCrFeNi high-entropy alloy. Scr. Mater. 139:49–52.

[16] Lv Y., Hu R., Yao Z., Chen J., Xu D., Liu Y., and Fan X. (2017) Cooling rate effect on microstructure and mechanical properties of AlxCoCrFeNi high entropy alloys. Mater. Des. 132: 392–399.

[16] Zhang Y., Zhou Y.J., Lin J.P., Chen G.L., and Liaw P.K. (2008) Solid-solution phase formation rules for multi-component alloys. Adv. Eng. Mater. 10(6): 534–538.

[17] Qiao J.W., Ma S.G., Huang E.W., Chuang C.P., Liaw P.K., and Zhang Y. (2011) Microstructural Characteristics and Mechanical Behaviors of AlCoCrFeNi High-Entropy Alloys at Ambient and Cryogenic Temperatures. Mater. Sci. Forum 688:419–425.

[18] Wells A.F. (1984) Structural Inorganic Chemistry 5th ed. Clarendon Press Oxford.

[19] Lifshitz I.M. and Slyozov V.V. (1961) The kinetics of precipitation from supersaturated solid solutions. J. Phys. Chem. Solids 19(1-2):35–50.

[20] Nadutov V.M., Mazanko V.F., and Makarenko S.Y. (2017) Tracer diffusion of cobalt in high-entropy alloys. AlхFeNiCoCuCrMetallofiz. Noveishie Tekhnol. 39(3):337–348.

[21] Chang S.Y., Li C.E., Huang Y.C., Hsu H.F., Yeh J.W., and Lin S.J. (2014) Structural and thermodynamic factors of suppressed interdiffusion kinetics in multi-component high-entropy materials. Sci. Rep. 4:4162.

[22] Hancock G.F. and McDonnell B.R. (1971) Diffusion in the intermetallic compound NiAl. Phys Stat Sol (a) 4(1):143-150.

[23] Li C, Li JC, Zhao M, and Jiang Q (2010) Effect of aluminum contents on microstructure and properties of AlxCoCrFeNi alloys. J. Alloys Compd. 504S:515–518.

# [24] Tang Z., Senkov O.N., Parish C.M., Zhang C., Zhang F., Santodonato L.J., Wang G., Zhao G., Yang F., and Liawa P.K. (2015) Tensile ductility of an AlCoCrFeNi multi-phase high-entropy alloy through hot isostatic pressing (HIP) and homogenization. Mater. Sci. Eng. A 647:229–240.

# [25] Nair R.B., Arora H.S., Mandal P., and Grewal H.S. (2018) Complex concentrated coatings: effect of processing route on microstructural and mechanical properties. Mater. Lett. 230:100–104.

[26] Yang T., Xia S., Liu S., Wang C., Liu S., Fang Y., Zhang Y., Xue J., Yan S., and Wang Y. (2016) Precipitation behavior of AlxCoCrFeNi high entropy alloys under ion irradiation. Sci. Rep. 6:32146.

[27] Chou H.P., Chang Y.S., Chen S.K., and Yeh J.W. (2009) Microstructure, thermophysical and electrical properties in AlxCoCrFeNi (0 ≤ x ≤2) high-entropy alloys. Mater. Sci. Eng. B 163(3):184–189.