Chapter 4: Dynamic indentation modulus of viscoelastic films

In this chapter, we employ theoretical modelling, theoretical formulations, and numerical simulations to identify semi-empirical relationships between the dynamic indentation modulus of viscoelastic films to the dynamic modulus film-substrate laminates. Accordingly, we introduce an analytical-experimental methodology that enables to back-calculate the dynamic modulus of the pristine film from dynamic indentation measurements on the whole laminate.

  - Viscoelastic film on an infinitely rigid substrate

We consider a viscoelastic film of thickness H and dynamic (complex) modulus Ef*=Ef'+j⋅Ef'' overlays a rigid and massive substrate; Ef' and Ef'' are, respectively, the storage and loss  moduli of the film, Ef=Ef'2+Ef''2 is the modulus magnitude of the film, and tanδf=Ef''/Ef' is the loss coefficient of the film. This film-substrate laminate experiences an indentation by a rigid axisymmetric tip that forms a circular contact area of radius a with the film (Figure 1a). The ratio H/a indicates the indentation state of the film; H/a≫1 represents narrow-contact indentations of an ultra-thick film, H/a≪1 represents broad-contact indentations of an ultra-thin film, and H/a≈1 represents moderate-contact indentations of a moderate-thick film (Figure 1b-c). At this indentation state, the laminate undergoes a refined dynamic indentation testing that yields the dynamic modulus of the film-substrate laminate EL*=EL'+j⋅EL'', where  EL' and EL'' are, respectively, the storage and loss parts of the laminate modulus, EL=EL'2+EL''2 is the modulus magnitude of the laminate, and tanδL=EL''/EL' is the loss coefficient of the laminate. To identify the relationships between the dynamic modulus of the film-substrate laminate (EL*) and the dynamic modulus of the pristine film (Ef*), we employ dynamic indentation Finite Element simulations on film-substrate laminates with various film characteristics (thickness H, modulus magnitude Ef, and loss coefficient tanδL), different tip shapes (spherical, conical, and flat), and different tip–film contract radii (a). Briefly, (1) we apply an initial indentation into the film and extracted the resultant contact area; (2) we generate additional, much smaller, harmonic variations in the tip depth and extracted the resultant harmonic reaction force on the tip; (3) we calculate the amplitude-ratio and phase-shift between the harmonic force and depth signals of the tip and calculate the dynamic stiffness contact; (4) we use the fundamental formulations of indentation mechanics to extract EL* from the contact complex stiffness and contact radius measures (see Appendix for more details).

Fig. 1. (a) Schematic description of an dynamic indentation into a viscoelastic film (dynamic modulus Ef*, thickness H) overlays an infinitely rigid substrate. The model comprises a viscoelastic film. A rigid indentation tip penetrates the film region of the film-substrate laminate and forms a circular contact area of radius a with the film. (b) Schematic illustrations of indentation states of the film, indicated by the geometrical ratio of the film thickness, divided by the contact area radius (H/a=2.73, 1.09, 0.54); the states are demonstrated by a spherical tip. (c) Schematic illustrations of a certain indentation state, H/a=2,  achieved by different axisymmetric tip shapes (from left to right: conical, spherical, and flat).

At the first stage, we analyze the mechanical response of the laminate to a spherical indentation tip and analyze the variations in the resultant dynamic modulus of the laminate modulus, normalized by the film modulus magnitude (EL*/Ef)—for a range of indentation states parameters (H/a), and selected film loss coefficients that span the typical range of viscoelastic materials (tanδf=0.1,0.3,0.5) (Figure 2). The normalized storage and loss moduli of the laminate (EL'/Ef and EL''/Ef) substantially vary with the indentation state parameter (H/a), and with the loss coefficient of the film (tanδf) (Figure 2a-b). Both EL'/Ef and EL''/Ef diverge toward H/a≪1, monotonically decrease as H/a increases, and approach asymptotically to the film characteristics for H/a≫1, namely,  EL'/Ef(H/a≫1)→Ef'/Ef and EL''/Ef(H/a≫1)→Ef''/Ef. Additionally, loss coefficient of the film (tanδf) distinguishes the results of EL'/Ef (or EL''/Ef) from one another, where the ratio between data sets with different tanδf values preserve along the entire H/a range. Next, we express the results in Figure 2a-b by the normalized modulus magnitude of the laminate (EL/Ef) (Figure 2c), for which all data sets coincide into a single form that characterized by an indentation shape function ϕ(H/a):

ELEf=1ϕ(H/a)               	(1)

In the limit of H/a→∞ ,the indentation state corresponds to that of a semi-infinite film, for which the laminate modulus approaches to that of the pristine film, EL→Ef, and the indentation shape function approaches unity, ϕ(H/a→∞ )→1; in the limit of H/a→0, the indentation state corresponds to that of a semi-infinite rigid substrate, for which laminate modulus approaches to that of the rigid substrate, EL→∞, and the indentation shape function approaches zero, ϕ(H/a→0 )→0. To complement these observations, we express the results in Figure 2a-b by the loss coefficient of the laminate, normalized by the loss coefficient of the film (tanδL/tanδf); this loss coefficient ratio equals unity for all H/a range analyzed:

tanδLtanδf=1             	(2)

Fig. 2. The dynamic modulus of laminates with viscoelastic films and rigid substrates. Variations in the normalized laminate modulus (EL*/Ef) for a range of indentation states parameters (H/a), and selected film loss coefficients (tanδf=0.1,0.3,0.5). Symbols indicate the FE results, and the lines indicates their analytical fitting. (a) EL'/Ef ratio (b) EL''/Ef ratio (c) EL/Ef ratio and tanδL/tanδf ratio. Note the log scale in the horizontal axis.

At the next stage, we extend FE dynamic indentation analysis of the laminate to other tip geometries (conical and flat), combine them with the former results for spherical tips, and plot the variations in the film-to-laminate modulus magnitude ratio and loss coefficient ratio,  Ef/EL and tanδL/tanδf, with the indentation state parameter H/a for the entire data set (Figure 3). Consequentially, we identify that the loss coefficient of the laminate equals to that for the film  tanδf=tanδL, regardless the specific tip geometry and the indentation state parameter; we also identify that the indentation shape function is only minorly affected by the specific tip geometry, and can be expressed analytically via Weibull’s function:

ϕHa=1-exp-1λ⋅Haβ       ;     λ=1.7   and  β=0.6               	(3)

By combining the above outcomes, we draw the following relationship between the dynamic modulus of the film-substrate laminate (EL*) and the dynamic modulus of the pristine film (Ef*):

Ef*=EL*⋅ϕ(Ha)               	(4)

Practically, Eq. (4) indicates that an unknown film dynamic modulus directly extracted from a conventional dynamic indentation testing of the film-substrate laminate, simply by linear scaling of resultant laminate dynamic modulus via the indentation shape function ϕ(H/a). We elaborate on this aspect later in the context of viscoelastic film on an elastic substrate.

Fig. 3. The dynamic modulus of laminates with viscoelastic films and rigid substrates for different axisymmetric tip shapes. Variations in the film-to-laminate modulus magnitude ratio and loss coefficient ratio,  Ef/EL and tanδf/tanδL for a range of indentation states parameters (H/a), and representative film loss coefficient tanδf=0.5; analyzed for a viscoelastic film on an infinitely rigid substrate, with different tip geometries (spherical conical and flat). Symbols indicate the FE results, and the lines indicates their analytical fitting for the indentation shape function ϕ(H/a).

  - Viscoelastic film on an elastic substrate

    - Theoretical modeling and analytical relationships

We now consider a viscoelastic film of thickness H and dynamic modulus Ef* overlays an elastic substrate of elastic modulus Es. We model the mechanical response of this viscoelastic–elastic laminate as a pair of springs in a series—a complex spring for the film, followed by an elastic film to the substrate—weighted by the indentation shape function  ϕ(H/a) (Figure 4). Accordingly, we link the laminate dynamic modulus EL* to the film dynamic modulus Ef* and the substrate elastic modulus Es via the weighted inverse rule-of-mixtures:

1EL*=ϕEf*+1-ϕEs               	(5)

Notably, Eq. (5) approaches the physical limits of EL*=Ef* for ϕ=1 (semi-infinite film) and EL*=Es for ϕ→0 (semi-infinite substrate), and degenerates into Eq. (4) for Es→∞ (infinitely rigid substrate). To obtain explicit analytical relationships between the storage and loss moduli of the laminate, to the storage and loss moduli of the film and the elastic modulus of the substrate, we substitute EL*=EL'+j⋅EL'' and  Ef*=Ef'+j⋅Ej''  into Eq. (5), separate into real and imaginary parts, and solve for EL', and EL'' that yields.

EL'=Es⋅Ef'2⋅1-ϕ+Ef'⋅Es⋅ϕ+Ef''2⋅1-ϕEf'2⋅1-ϕ2+2⋅Ef'⋅Es⋅ϕ⋅1-ϕ+Ef''2⋅1-ϕ2+Es2⋅ϕ2	(6)

EL''=Ef''⋅Es2⋅ϕEf'2⋅1-ϕ2+2⋅Ef'⋅Es⋅ϕ⋅1-ϕ+Ef''2⋅1-ϕ2+Es2⋅ϕ2	(7)

Then, we divide the nominator and denominator of Eqs. (6-7) by ϕ⋅Es2, extract Ef' from the nominator of Eq. (6), extract Ef'' from the nominator of Eq. (7), and rearrange them into the following:

EL'=Ef'⋅1ϕ⋅AB	(8)

EL''=Ef''⋅1ϕ⋅1B	(9)

with

A=Ef'2+Ef''2Ef'⋅Es⋅1-ϕϕ+1	(10a)

B=Ef'2+Ef''2Es2⋅1-ϕϕ2+2⋅Ef'Es⋅1-ϕϕ+1	(10b)

Next, we proceed to express the analytical relationships between the modulus magnitude and loss coefficient of the laminate, the modulus magnitude and loss coefficient of the film, and the elastic modulus of the substrate. Firstly, we introduce Eqs. (8–9) into EL=EL'2+EL''2, identify that Ef''/Ef=11+1/tan2δf, and apply some algebra, which yields:

EL=Ef⋅1ϕ⋅AB⋅1+11+1/tan2δf⋅1-A2A2	(11)

Secondly, we introduce Eqs. (8-9) into tanδL=EL''/EL', which directly yields:

tanδL=tanδf⋅1A	(12)

Thirdly, we express Eqs. (10a–10b) via Ef=Ef'2+Ef''2 and tanδf=Ef''/Ef', and apply some algebra, which yield:

A=EfEs⋅1-ϕϕ⋅1+tan2δf+1	(13a)

B=EfEs2⋅1-ϕϕ2+2⋅EfEs⋅11+tan2δf⋅1-ϕϕ+1	(13b)

Fig. 4. Viscoelastic film (dynamic modulus Ef*, thickness H) overlays an elastic substrate (elastic modulus Es)—modeled as a pair of springs in a series.

To analyze the validity of the theoretical relationships in Eqs. (8–13), we extend our FE analysis for laminates of films and elastic substrates—indicated via the film-to-substrate modulus ratio Ef/Es (see appendix for details). We analyze the variations in the laminate storage and loss moduli (EL' and EL''), and the laminate modulus magnitude and loss coefficient (EL and tanδL) for a range indentation states of the film (H/a), and a set of film-to-substrate moduli (Ef/Es=1, 1/3, 1/5, 1/10, 1/100), and two film loss coefficients (tanδf=0.1 and tanδf=0.5)  (Figures 5–6). We plot the FE results for the normalized laminate storage and loss moduli (EL'/Ef and EL''/Ef) with the analytical predictions of Eqs. (8–9) (Figure 5a–5b for tanδf=0.1; Figure 6a–6b for tanδf=0.5), and we plot the normalized laminate modulus magnitude (EL/Ef) and normalized loss coefficient (tanδL/tanδf) with the analytical predictions of Eqs. (11–12) (Figure 5c-5d for tanδf=0.1; Figure 6c-6d for tanδf=0.5); for all calculations we used the shape function in Eq. (3), and the A and B expressions in Eqs. (13a–b). Notably, the proposed spring-series model and its resultant theoretical relationships agree well with the FE results for the entire parameter–range analyzed. For Ef/Es=1/100 all parameters of the laminate dynamic modulus lay closely to that of asymptotic, infinitely rigid substrate case, and only small differences are observed below H/a~0.1. As Ef/Es increases the effect of the elastic substrate becomes more pronounced, which yields a progressive reduction in EL'/Ef, EL''/Ef, EL/Ef, and tanδL/tanδf along the entire H/a range compared to the case of an infinitely rigid substrate; this effect is more preannounced for smaller H/a ratios (e.g., thin-film laminates) and becomes minor for high H/a ratios (e.g., thick-film laminates). The case of Ef/Es=1 represents a special laminate configuration, in which the film modulus magnitude equals to the substrate elastic modulus. In this configuration, the laminate loss modulus and loss coefficient are extremely sensitive to variations in the indentation state parameter (H/a); specifically, for ultra-thin films (H/a≪1) the loss coefficient of the laminate becomes much smaller to that of the film tanδL≪tanδf, and accordingly viscosity effects of the laminate become negligible, such that  EL'/Ef≈EL/Ef→1, and EL''/Ef≪1.

Fig. 5.  The dynamic modulus of laminates with viscoelastic films and elastic substrates; theoretical modeling vs. FE simulations. Variations in the normalized laminate storage and loss moduli (EL'/Ef and EL''/Ef), and the laminate normalized modulus magnitude and loss coefficient (EL/Ef and tanδL/tanδf) for a range indentation states of the film (H/a), and a set of film-to-substrate moduli (Ef/Es=1, 1/3, 1/5, 1/10, 1/100), and film loss coefficients tanδf=0.1. Symbols indicate the FE results, and the lines indicates the analytical predictions. Note the log scale in the horizontal axis. (a-b) EL'/Ef and EL''/Ef ratio. The full and dashed lines indicate the analytical results of Eqs. (8-9) and (15-16) respectively. (c-d) EL/Ef and tanδL/tanδf ratio. The full and dashed lines indicate the analytical results of Eqs. (11-12) and (17-18) respectively.

Fig. 6. The dynamic modulus of laminates with viscoelastic films and elastic substrates; theoretical modeling vs. FE simulations. Variations in the normalized laminate storage and loss moduli (EL'/Ef and EL''/Ef), and the laminate normalized modulus magnitude and loss coefficient (EL/Ef and tanδL/tanδf) for a range indentation states of the film (H/a), and a set of film-to-substrate moduli (Ef/Es=1, 1/3, 1/5, 1/10, 1/100), and film loss coefficients tanδf=0.5. Symbols indicate the FE results, and the lines indicates the analytical predictions. Note the log scale in the horizontal axis. (a-b) EL'/Ef and EL''/Ef ratio. The full and dashed lines indicate the analytical results of Eqs. (8-9) and (15-16) respectively. (c-d) EL/Ef and tanδL/tanδf ratio. The full and dashed lines indicate the analytical results of Eqs. (11-12) and (17-18) respectively.

    - Simplified analytical relationships

Now, we focus our analysis on viscoelastic films with loss coefficients in an order of magnitude of tanδf~O0.1, as commonly appears in viscoelastic materials—and employ analytical approximations into Eqs. (8–9, 11–13) to identify simplified expressions for the laminate dynamic modulus. In this framework, we use the approximation 1+tan2δf=1+Otan2δf~1, and reduce A and B in Eqs. (13a–b) into:

C=EfEs⋅1-ϕϕ+1         ;         A=C    ,      B=C2     	(14a,b,c)

With these expressions, the laminate storage and loss modulus Eqs. (8–9) reduce into:

EL'=Ef'⋅1ϕ⋅1C	(15)

EL''=Ef''⋅1ϕ⋅1C2	(16)

Accordingly, we introduce Eqs. (14a–c) into the laminate modulus magnitude and loss coefficient expressions in Eq. (11–12), employ an analogous approximation for the root term in Eqs. (11), and obtain:

EL=Ef⋅1ϕ⋅1C	(17)

tanδL=tanδf⋅1C	(18)

Notably, with these approximations, we identify that all dynamic modulus characteristics of the laminate (EL',EL'',EL and tanδL) directly link to the corresponding characteristics of the film (Ef',Ef'',Ef and tanδf) via linear scaling—which depends only on the indentation states parameter (H/a) of the laminate, and the film-to-substrate modulus ratio (Ef/Es). For an increasing substrate stiffness, the Ef/Es decreases, and the effect of the substrate modulus on the laminate dynamic modulus decreases; in the asymptotic case of an infinitely rigid substrate (Es→ ∞) the effect of substrate modulus on the laminate dynamic modulus vanishes, C→1 and Eqs. (17–18) degenerate into the relationships of Eqs. (1–2).

To verify the adequacy of the approximated formulae in Eqs. (14–18), we plotted their predictions with those of the corresponding non-approximated expressions in Eqs. (8–13), and with the FE results above—for a range indentation states of the film (H/a), and a set of film-to-substrate moduli (Ef/Es=1, 1/3 , 1/5, 1/10, 1/100), and two film loss coefficients (tanδf=0.1 and tanδf=0.5) (Figures 5–6). Evidently, for tanδf=0.5 the approximated formulae in Eqs. (14–18) closely follow the full expressions and the FE simulations with only slight deviations for H/a<1 ratios (Figures 5); for tanδf=0.1 the approximate expressions coincide with the full expressions and agree well with the FE simulations (Figures 6).

Functionally, the storage modulus ratio EL'/Ef' from Eq. (15) indicates the energy storage capabilities of the laminate, relative to that of the pristine viscoelastic film, and the loss modulus ratio EL''/Ef'' from Eq. (16) indicates the energy dissipation capabilities of the laminate, relative to that of the pristine viscoelastic film; we explicitly formulate these ratios as follows, and analyze their variations with the indentation state parameter through the shape function ϕ(H/a), and with the film-to-substrate modulus ratio (Ef/Es) (Figures 7):

EL'Ef'=1EfEs⋅1-ϕ+ϕ	(19)

EL''Ef''=1EfEs21ϕ⋅1-ϕ2+2⋅EfEs⋅1-ϕ+ϕ	(20)

For ultra-thick films ϕ(H/a≫1)→1 both EL'/Ef' and EL''/Ef'' approach unity, and the laminate energy storage and energy dissipation capabilities correspond to that of the pristine film. For ultra-thin films ϕH/a≪1≪1, the storage modulus ratio yields EL'/Ef'~Es/Ef⋅1-ϕ that which approaches to Ef/Es for H/a→0, and indicates that the energy storage of the film within the laminate is amplified by the substrate-to-film modulus ratio; accordingly, the loss modulus ratio yields EL''/Ef''~ϕ/Ef/Es2 that which approaches to zero for a finite-modulus substrate when H/a→0, and indicates that the energy dissipation capabilities of the film within in the laminate vanishes. The storage modulus ratio EL'/Ef' monotonically decreases from Es/Ef toward unity as H/a increases; for the specific case of Ef/Es=1, the EL'/Ef' ratio equals unity for the entire H/a range. The loss modulus ratio EL''/Ef'' rises from zero and approaches unity as H/a increases, and possibly reaches an extremum in between—which its location and magnitude depend on the Ef/Es ratio. To identify the characteristics of this extremum, we derive require zero for its the derivative, d(EL''/Ef'')/d(H/a)=0, which yields the that:

EL''Ef''max=1EfEs21ϕ⋅1-ϕ2+2⋅EfEs⋅1-ϕ+ϕ       	(21)

where ϕ is the shape function value that yields this extremum:

ϕ=EfEs⋅11-2⋅EfEs 	(22)

Notably, by introducing the constraint for the maximal possible value of the shape function ϕ≤1, we identify that an extremum can be achieved only film-to-substrate modulus ratio that satisfies Ef/Es<2-1. Finally, by using the explicit analytical form of the shape function from Eq. (3) into Eq. (18), we identify that the extremum is reached for an indentation shape parameter of:

Ha=λ⋅-ln1-EfEs⋅11-2⋅EfEs1β               ;     λ=1.7   and  β=0.6 	(23)

Fig. 7. The storage and loss moduli of laminates with viscoelastic films and elastic substrates. Variations in the storage modulus ratio (EL'/Ef') and the loss modulus ratio (EL''/Ef''), for a range indentation states of the film (H/a), and a set of film-to-substrate moduli (Ef/Es=1, 1/3, 1/5, 1/10), and film loss coefficients tanδf=0.5. Symbols indicate the FE results, and the lines indicates the analytical predictions. Note the log scale in the horizontal axis. (a) EL'/Ef' ratio. The lines indicate the analytical results of Eq. (19). (b) EL''/Ef'' ratio. The lines indicate the analytical results of Eq. (20).

  - Extracting the film dynamic modulus via dynamic indentation testing of a film-substrate laminate

With the analytical relationships in Eqs. (14–18), we approach to set analytical relationships to extract the modulus magnitude and loss coefficient of the film (Ef and tanδf) from the corresponding parameters of the laminate (EL and tanδL) that directly obtained from its dynamic indentation measurements. First, we substitute Eq. (14a) into Eq. (17), and explicitly express it as follows:

EL=Ef⋅1EfEs⋅1-ϕ+ϕ	(24)

Then, we use some algebra on Eq. (24) to express Ef as a function of ϕ, EL, and Es, which yields:

Ef=κE⋅EL              ;        κE=ϕ1-ELEs⋅1-ϕ	(25)

Next, we isolate 1/C from Eq. (17) and express it via Eq. (25):

1C=1κE⋅ϕ	(26)

Then, we introduce the relationship in Eq. (26) into Eq. (18), and express tanδf as a function of ϕ, EL, Es, and tanδL:

tanδf=κδ⋅tanδL              ;        κδ=11-ELEs⋅1-ϕ	(27)

Eqs. (25,27) show that the film–laminate modulus magnitude and loss coefficient characteristics, Ef–EL and tanδL–tanδf, link via linear scaling; the scaling factors, κE and κδ, depend only on the laminate-to-substrate modulus ratio (EL/Es), and the shape function that links to the indentation state parameter of the film (ϕ(H/a)). Specifically, when the laminate-to-substrate modulus ratio is sufficiently small (e.g., EL/Es<1/10), the denominators of κE and κδ approaches unity, and Eqs. (25,27) further simplify into Ef≈ϕ⋅EL and tanδf≈tanδL–which correspond to the results of a laminate with an infinitely rigid substrate Eqs. (1–2). Notably, as κE and κδ are nondimensional, the Ef–EL and tanδL–tanδf relationships in Eqs. (25,27) are independent of the absolute moduli magnitudes of the film and substrate— and are thus generally applicable for the broad dimensional range of laminates with mechanical characteristics, i.e., from highly rigid to substantially compliant, and from nearly elastic to prominently viscous.

To verify the linear relationships in Eq. (25,27), we applied FE simulations with a wide range of input film and substrate moduli, film thickness parameters, and different axisymmetric tip geometries (conical, spherical, and flat)—and plotted their resultant pairs Ef-EL pairs (Figure 8), and tanδf–tanδL pairs (Figure 9). For each simulation model, we extracted the indentation contact area radius (a), the laminate modulus magnitude (EL) and the laminate loss coefficient (tanδL)— and identified the shape function value via the indentation state parameter, resultant the laminate-to-substrate modulus ratio (EL/Es). Then, we calculated the film -laminate scaling factors (κE and κδ) and plotted the theoretical relationships in Eqs. (25,27) with direct results for the Ef-EL, and tanδf–tanδL pair sets from the numerical simulations (Figures 8–9)—which show excellent correspondence for the entire range of input parameters analyzed.

Fig. 8. The Ef-EL relationships for laminates at various indentation states (H/a=10,1,0.2), shown for Ef/Es=1/10,1/3, and tanδf=0.1,0.5. Symbols indicate the FE results, and the lines indicates the analytical results of Eq. (25) for each parameter group (i.e., Ef/Es, tanδf and H/a). (a) Ef-EL relationships shown for Ef/Es=1/10. (b) Ef-EL relationships shown for Ef/Es=1/3.

Fig. 9. The tanδf-tanδL relationships for laminates at various indentation states (H/a=10,1,0.2), shown for Ef/Es=1/10,1/3. Symbols indicate the FE results, and the lines indicates the analytical results of Eq. (27) for each parameter group (i.e., Ef/Es, and H/a). (a) tanδf-tanδL relationships shown for Ef/Es=1/10. (b) tanδf-tanδL relationships shown for Ef/Es=1/3.

Having validated the film–laminate relationships in Eqs. (25,27), we can propose the following analytical–experimental methodological approach to back-calculate the film dynamic modulus from dynamic indentation measurements on the laminate.

Step 1: Use microscopy observations to identify the thickness of the film within the laminate (H).

Step 2: Use mechanical testing (or literature data) to determine elastic modulus of substrate within the laminate (Es).

Step 3: Apply standard dynamic indentation testing on the laminate, identify the tip-film contact radius (a), and extract the modulus magnitude and loss coefficient of the laminate (EL and tanδL).

Step 4: Calculate film -laminate scaling factors (κE and κδ, via Eqs. (25,27)), and use them to back-calculate the film modulus magnitude and loss coefficient (via Ef=κE⋅EL, and tanδf=κδ⋅tanδL).

Practically, the estimations of H/a and EL/Es typically incorporate a certain deviation range, which arise from resolution limitation of the microscopy analysis, from measurement errors of the contact radius, and measurement errors of the mechanical testing, such that H/a →H/a ±ΔH/a, and EL/Es→EL/Es±ΔEL/Es.  Accordingly, the film -laminate scaling factors also include deviation ranges, κE→κE±ΔκE, and κδ→κδ±Δκδ, such that Ef→ Ef± ΔEf and tanδf→ tanδf± Δtanδf, where:

ΔEf=±ΔκE⋅EL              	(28)

Δtanδf=±Δκδ⋅tanδL              	(29)

To identify these deviations, we calculated the first-order differentials of Eqs. (25,27), namely ΔκE=dκE/d(H/a)⋅ΔH/a +dκE/d(EL/Es)⋅ΔEL/Es , and Δκδ=dκδ/d(H/a)⋅ΔH/a +dκδ/d(EL/Es)⋅ΔEL/Es , and expressed them analytically as follows:

ΔkEκE=β1-ϕ1λ⋅Haβ1-ELEsϕ1-ELEs⋅1-ϕ⋅ΔHaHa+1-ϕELEs1-ELEs⋅1-ϕ⋅ΔELEsELEs                           	(30)

Δκδκδ=-ELEsβ1-ϕ1λ⋅Haβ1-ELEs⋅1-ϕ⋅ΔHaHa+1-ϕELEs1-ELEs⋅1-ϕ⋅ΔELEsELEs                       	(31)

Notably, when the film modulus magnitude approaches the substrate elastic modulus (EL/Es→1), the κE deviations reduce into ΔκE≈κE⋅1-ϕEL/Es1-EL/Es⋅1-ϕ⋅ΔEL/EsEL/Es, namely they are  insensitive to H/a deviations. Moreover, for ultra-thin films (Ha≪1), the κE and κδ deviations further simplify into ΔκE≈κE⋅EL/Es1-EL/Es⋅ΔEL/EsEL/Es, and Δκδ≈κδ⋅EL/Es1-EL/Es⋅ΔEL/EsEL/Es, they are are insensitive to H/a deviations.

Appendix. Finite Element simulations of dynamic indentations of laminates with viscoelastic films overlay rigid and elastic substrates

We analyzed the dynamic indentation response of laminate with viscoelastic films overlay rigid or elastic substrates via commercial FE software ABAQUS/explicit (ver. 6.19) [D5-D6]. Perfect binding conditions were assumed between the discrete material phases. The bottom face of the phased model was fixed, while the lateral faces were kept free from mechanical loads. In addition, axisymmetric boundary condition was applied to the model axis. The outer surface area of the indenter was also fixed in the plane perpendicular to the force line of action, such that the indenter was unable to move or rotate horizontally. The model dimensions were chosen to be sufficiently large to avoid undesired effects by the boundary conditions. A frictionless contact between the indenter and the layered model were considered. The simulations included two loading steps, an initial quasi-static indentation (DC step), followed by an additional dynamic indentation (AC step). For the DC step, a quasi-static two-dimensional indentation models were used to analyze the indentation behaviour of the laminate (figure 1a and figure 4). Due to rotational symmetry in loading conditions and structure, only half of the composite system was modelled. The tip was modelled as a perfectly rigid element (spherical, conical and flat punch shape). The laminate was modelled as a two-dimensional solid, composed of two material regions, substrate, and film. The two regions were isotropic materials with an elastic–perfectly plastic constitutive behaviour. We modeled the mechanical response of the substrate and the film, respectively, via their indentation hardness parameters Hs and Hf. The hardness-to-modulus ratios Hs/Es and Hf/Ef characterize the onset of indentation damage in the substrate and film, respectively; as universally observed across a diversity of biomaterial-science studies these ratios Hs/Es≈Hf/Ef≈0.05 [Lebonet, Miserez- Property maps for abrasion resistance of materials]. Axisymmetric mesh elements were used (realized via axisymmetric, 4-node, reduced integration quadrilateral elements with hourglass control; CAX4R in ABAQUS element library). In the analysis of the film on a rigid substrate, the upper edge of the substrate was fixed. Non-uniform segmentation with a finer mesh in the vicinity of the indentation regime, was used to increase the solution accuracy at the region of interest. Mesh convergence was pre-analyzed to estimate the required mesh parameters. To incorporate nonlinear effects of large deformations and plasticity, we employed adaptive meshing (ALE method) to reduce element distortion effects. From each quasi-static simulation, the contact force was recorded in order to extract the contact radius (a) at the point of maximum depth. For the AC step, linear-elastic constitutive behaviour was used for the substrate material, frequency domain viscoelastic constitutive behaviour was used for the viscoelastic film. Axisymmetric mesh elements were used (realized via axisymmetric, 4-node, quadrilateral elements with hybrid formulation; CAX4H in ABAQUS element library). The element in contact (extracted using the contact radius from the DC step) were loaded by a uniformly distributed axial harmonic displacement with fixed amplitude (u), which accommodates the use of a direct-solution steady-state dynamic analysis. From each harmonic simulation, the real and imaginary part of the reaction force (P*) were recorded in order to extract EL and tanδL of each composite system. Specifically, the dynamic indentation modulus of the laminate is calculated via EL*=P*2au [*]. Note that the modulus magnitude of the laminate is the magnitude of EL* (namely, EL=EL*), while the loss coefficient of the laminate is obtained by dividing the real and imagine parts of EL* (tanδL=I(EL*)/R(EL*)), which is the ratio between the loss modulus and storage modulus. The storage and loss moduli of the laminate is obtained from the real and imagine parts of EL* (namely, EL'=REL*, EL''=IEL*).