Abstract

The surface chemistry of stimulus-responsive nanoparticles plays an important role in mediating nano-bio interactions in cancer nanomedicine by targeting the unique features of the tumor microenvironment, such as low extracelullar pH. To develop therapeutic nanoparticles with high sensitivity and instant response to subtle pH differences in the systemic circulation, we produced a novel polyzwitterion with acylsulfonamide-based betaine structure by one-step modification of polycarboxybetaine (PCB) with benzene sulfonamide. The zwitterionic micellar shells show high antifouling in the blood circulation and acutely convert into positive charge via acylsulfonamide protonation, thereby improving cell affinity at tumor sites. Moreover, a disulfide bond between the shell and poly-ε-caprolactone (PCL) core allows for reductive-responsive release of doxorubicin (DOX) after internalization of the polymeric micelles. Finally, in vitro and in vivo competition assays demonstrated that dual responsive drug-loaded micelles have better anticancer efficiency than free DOX or micelles without zwitterionic pH-responsive properties. Thus, we have developed a simple and valuable strategy to enhance pH sensitivity of micellar carriers for cancer treatment.

Key words: acylsulfonamide, pH sensitivity, disulfide-bonded, charge reversal, cancer treatment.

Introduction

Nanoparticle (NP)-based drug delivery systems (NDDS) have been intensively explored over the past decades to modify the pharmacokinetics and biodistribution of antitumor drugs, leading to significant clinical breakthroughs [1, 2]. However, the delivery efficiency of most NPs developed to date remains relatively low, which limits their clinical application [3]. Complex physiological barriers and nonspecific interactions are major factors hindering the efficient transport and delivery of therapeutic NPs [4]. To address these challenges, significant efforts have been invested into the development of intelligent NDDS targeting the tumor microenvironment [5]. For instance, various responsive polymer micelles self-assembled from block copolymers have been formulated to target tumor extracellular biochemical properties such as hypoxia, acidity, and specific enzymes, and have shown strong therapeutic potential [6-8]. However, these biochemical properties are often heterogeneous or based on subtle differences from normal tissue. Thus, responsive NPs targeting the tumor microenvironment must have high sensitivity to improve targeting accuracy and minimize side effects[9].

In most solid tumors, the extracellular pH (pHe) is more acidic than that of normal tissues due to the Warburg effect [10]. NPs with conversional surface chemistry are efficient, versatile therapeutic tools that take advantage of this pH variation to facilitate cellular uptake and enhance antitumor efficacy [11]. Typically, neutral or negative NPs are able to reduce undesired interactions in the bloodstream and thereby ensure a prolonged circulation time. When they reach a tumor, NPs switch their surface potential into positive charge upon acidic stimuli, which gives them high affinity for pathological sites via electrostatic attraction[12]. Although several strategies have been explored for developing pH-responsive NPs, they present some disadvantages. For instance, an acid-cleavable unit can trigger chemical deprotection and exposes cationic groups of NPs [13], yet the cleavage reaction is gradual and difficult to control in a narrow acidic gradient (from 7.4 to 6.5). Alternatively, polymers with weak basic groups, such as polyhistidine or poly(β-amino ester), can promote the cationization of therapeutic NPs at acidic pHe via protonation of the basic group [14]. However, the deprotonated state in the bloodstream is hydrophobic and enveloped in the carrier’s core. The circulation stability of this system therefore relies on an additional hydrophilic polymer, such as polyethylene glycol (PEG), which may cause charge shielding effects at tumor sites and consequently inhibit endocytosis in cancer cells[15].

Zwitterionic polymers (polyzwitterions) have a unique structure with equal number of cationic and anionic groups on the molecular chains, which makes them neutral and highly hydrophilic [16]. Due to these physical properties, polyzwitterions have ultra-high resistance to protein adsorption, excellent biocompatibility, and undetectable immune response, and therefore represent a viable alternative to PEG in drug delivery systems [17, 18]. Additionally, the structure of zwitterionic polymers allows for straightforward charge transitions by selectively reducing or increasing an ion pair[19]. For instance, in quantum dots coated with a pHe-responsive polyzwitterion with an ethylenediamine-based betaine structure[20], a di-protonation process converts the neutral net charge of pH 7.4 into cationic at tumor pHe, resulting in enhanced antifouling and increased tumor accumulation. Moreover, the pKa of sulfonamide derivatives is within the physiological pH range[21-23]. Rotello‘s group creatively introduced an acylsulfonamide group as anionic moiety in zwitterionic ligands, and showed that an acute charge transition of zwitterionic gold NPs occurred at tumor pHe [24]. Analogous zwitterionic micelles formed by self-assembly of mixed-charged copolymers also showed pHe-responsive drug delivery and positive cancer treatment positive outcomes [25-27], and their surface chemistry depended on complex structural regulation. Thus, pH-responsive polyzwitterions represent a promising mechanism to selectively mediate nano-bio interactions between circulation and tumor sites for improved clinical applications in cancer nanomedicine.

The therapeutic efficacy of NDDS is highly dependent on their capacity for intracellular payload release. However, drug permeation also relies on hydrophobicity[28]. An efficient strategy to improve NDDS drug intracellular release involves introducing disulfide bonds to trigger demicellization or degradation in high glutathione intracellular levels [29]. In the present study, we developed a novel polymer micelle system with a pHe-responsive polyzwitterion shell and a disulfide-linked biodegradable poly-ε-caprolactone core, for improving delivery and release of anticancer drugs in vitro and in vivo (Scheme 1). The acylsulfonamide betaine structure on the polyzwitterion shell provides the micellar nanocarrier with a sensitive and reversible surface charge-conversion mechanism via protonation/deprotonation in acidic tumor microenvironments. Thus, this novel micellar carrier possesses excellent antifouling in the blood circulation and activatable uptake by cancer cells after accumulating at tumor sites by EPR effect. The intracellular release of doxorubicin is accelerated by reductive responsiveness.

Scheme 1. Schematic representation of the micellar carrier structure and in-vivo delivery of DOX into cancer cells.

- Experimental Section

  - Materials

A zwitterionic triblock copolymer containing a disulfide-linked poly-ε-caprolactone and polycarboxybetaine methacrylate (PCB-SS-PCL-SS-PCB) was prepared by RAFT polymerization of carboxybetaine methacrylate by using a PCL-RAFT macromolecular chain transfer agent containing cystamine units. The detailed synthesis and characterization of this polymer has been described in our previous report[30]. N-(3-Dimethylaminopropyl)-N'-ethyl carbodiimide hydrochloride (EDC•HCl, 98%) and N-Hydroxysuccinimide (NHS, 98%) were purchased from J&K Chemical, (Beijing, China) and used as received. Galactosamine (GAL) was purchased from Sigma-Aldrich (Shanghai, China). All other reagents and solvents were of analytical grade and used as received. Dulbecco’s modiﬁed Eagle’s medium (DMEM), penicillin-streptomycin, fetal bovine serum (FBS) and 3-[4, 5-dimethylthiazol-2-yl]-2, 5-diphenyltetrazolium bromide (MTT), were purchased from Thermo Fisher Scientific.

  - Modification of PCB-SS-PCL-SS-PCB with benzene sulfonamide

Benzene sulfonamide was used to modify the carboxylate group of PCB via EDC/NHS chemistry. To conjugate benzene sulfonamide, 10 mg of PCB-SS-PCL-SS-PCB were first incubated with 400 mM EDC and 200 mM NHS in mixed water and a DMSO solution for 30 min. After that, the pH value of the solution was maintained at pH 9 by using sodium borate buffer, and then reacted with 5 mg of benzene sulfonamide at RT for 4 h. The reacted solution was shifted to a dialysis bag (MWCO 7000) against deionized water to remove salt and unreacted benzene sulfonamide. Finally, benzene sulfonamide modified PCB-SS-PCL-SS-PCB (PCBSA-SS-PCL-SS-PCBSA) was obtained by freeze drying (8.8 mg, 82%).

Preparation and characterization of PCBSA Micelles

PCBSA-SS-PCL-SS-PCBSA (10 mg) was firstly dissolved in DMSO (2 mL) to prepare polymer solution with an initial concentration of 5.0 mg/mL. Subsequently, PB (50 mM, pH 7.4) was added to the polymer solution at a rate of 1 drop every 6-7 s under vigorous stirring until turbidity appeared in the solution, indicating the occurrence of micellization of PCBSA-SS-PCL-SS-PCBSA. The micelle solution was allowed to cool overnight and then transferred into a dialysis bag (MWCO 3500) against PB for 48 h to remove DMSO. Finally, the PCBSA-SS-PCL-SS-PCBSA micelle (PCBSA micelles) solution was diluted to 0.2 mg/mL of polymer concentration.

The critical micelle concentration (CMC) of PCBSA micelles was determined by using pyrene as a fluorescence probe on a Varian fluorescence spectrophotometer at room temperature. The concentration of PCBSA-SS-PCL-SS-PCBSA varied from 2×10-4 to 0.2 mg/mL in water and the concentration of pyrene was fixed at 0.6 µM. The fluorescence spectra were recorded using a FLS920 fluorescence spectrometer with the excitation wavelength of 330 nm. The emission fluorescence was monitored at 368 nm and 375 nm. The CMC was estimated as the cross-point when extrapolating the intensity ratio I375/I368 at low and high concentration regions. The size distribution (PDI) of the micelles was measured using a laser particle size analyzer (Zetasizer Nano, Malvern, UK). Micellar morphology was observed under a Hitachi H600 transmission electron microscopy (TEM) system at an operated voltage of 75 kV. For TEM measurement, the sample was prepared by adding a drop of micelle solution onto the copper grid, and then the sample was air-dried and measured at room temperature. The preparation and characterization of PCB-SS-PCL-SS-PCB micelles (PCB micelles) were carried out following the same procedure used for PCBSA micelles.

  - DOX loading and release

A stock solution of the hydrophobic drug DOX was prepared by mixing DOX·HCl with TEA in dimethyl sulfoxide (DMSO) for 2 h. Subsequently, 2 mL DOX solution (1 mg/mL) was added into a bottle with 10 mg PCBSA-SS-PCL-SS-PCBSA. After stirring overnight, PB (50 mM, pH 7.4) was added to the above solution at a rate of 1 drop every 6-7s until the formation of micelles. The solution was transferred into a dialysis bag (MWCO 3500) against PB for 48 h, and then filtered through a 0.45µm filter to remove the unloaded DOX. DOX-loaded micelles were lyophilized and resolved in DMSO for determination of drug loading content (DLC) and drug loading efficiency (DLE) by using a UV-Vis spectrophotometer (absorbance intensity at 485 nm). DLC and DLE were calculated using the following equations:

in vitro DOX release profiles were investigated using a dialysis tube (MWCO 14000) at 37 °C against PB (50 mM) at pH 7.4 in the absence or presence of 10 Mm and 10 mM GSH. At regular time intervals, 3 mL of release media was taken out and replaced with an equal volume of fresh media. The amount of DOX released from the polymeric micelles was determined by UV-vis spectroscopy (Agilent Technologies). These release experiments were conducted in triplicate, and the results presented correspond to the average data with standard deviations.

  - Cell Viability Assays

The cytotoxic effects of blank micelles, free DOX, and DOX-loaded micelles were determined with MTT assays. HepG2 cells were seeded into 96-well plates at 5000 cells/well and cultured for 24 h in 200 µl DMEM containing 10% FBS. The culture medium was replaced with 200 µl neutral medium (pH 7.4) and acidic medium (pH 6.5) containing the above formulations, respectively. After incubated for another 24 h, the medium was replaced with 200 µl of fresh medium. MTT (20 µl, 5 mg/ml in PBS) stock solution was then added to each well. After 4 h, unreacted dye was carefully removed, and the formazan crystals were dissolved to 200 µl/well DMSO. The plate was incubated for another 10 min before using absorbance at 570 nm to measure by an ELISA microplate reader (Bio-Rad). Cell viability (%) was calculated as: cell viability (%) = (ODsample/ODcontrol)∙100, where ODsample is the absorbance of the cells treated by polymers, and ODcontrol is the absorbance of the untreated cells. Each experiment was done in triplicate.

  - Cell Uptake Studies

HepG2 cells were seeded into 24-well plates at an initial density of 5∙104 cells/well with 1 mL DMEM containing 10% FBS and incubated at 37◦C for 24 h in 5% CO2. After reaching about 80% confluence, the medium was replaced with fresh medium (pH 7.4 or 6.5) containing DOX, DOX-loaded PCB micelles or DOX-loaded PCBSA with DOX concentration of 5 g/mL. After the desired incubation time, the cells were washed three times with PBS and then observed by fluorescence microscope. Thereafter, the cells were detached with 0.25% trypsin and then resuspended with 500 µl PBS (pH 7.4) for measurement with a flow cytometer (FC500, Beckman Coulter).

  - Blood Circulation and Biodistribution Studies

Adult SD rats (200 ± 20g) were randomly divided into three groups. DOX, DOX-loaded PCB micelles, or DOX-loaded PCBSA micelles at an equivalent DOX dose of 4 mg/kg were injected via the tail vein. 0.5 mL of blood were collected from the orbit sinus at different time points post-injection. The plasma was separated by centrifugation (3500 rpm, 10 min) and the supernatant was diluted in methanol containing 0.01 M HCl to precipitate proteins. After centrifuging twice (12000 rpm, 5 min), the supernatant was collected and dried by vacuum drying. The residue was dissolved in 0.5 mL of acetonitrile and water (50:50, v/v) and filtered with an ultrafiltration membrane (220 nm) for HPLC analysis.

The nude mice bearing HepG2 tumor was used for biodistribution studies. When tumor size reached 50 mm3, the mice were randomly divided into four groups with five animals per group. Tumor-bearing mice were intravenously injected with 200 µL of DOX, DOX-loaded PCB micelles, or DOX-loaded PCBSA micelles at an equivalent DOX dose of 4 mg/kg. After 12 h, the mice were sacrificed and their important organs (heart, liver, spleen, lung and kidney) and tumors were harvested, washed with cold saline, dried by filter paper and weighed. Subsequently, the organs and tumors were homogenized and extracted with DMSO containing 0.01 M HCl. After centrifuging and drying the organic phase, the corresponding DOX concentration was determined by HPLC analysis.

  - In vivo Antitumor Study

All animal experiments were conducted using protocols approved by the Ethics Committee of HAUST. For established xenografted human liver tumors, adult (10-12 weeks) male C57BL/6 mice received a subcutaneous inoculation of 100 µL mixture of 1×106 HepG2 cells and growth factor (1: 1) in the flank region. After tumor size reached 50 mm3, the mice were randomly divided into four groups with five animals per group. Mice were injected via the tail vein with 200 µL PBS, DOX, DOX-loaded micelles, or DOX-loaded GAL-Micelles at an equivalent DOX dose of 4 mg/kg every two days. Mice tumor size and body weight were measured before each injection. Tumor size was measured using vernier calipers and calculated using the following formula: V = d2×D/2 (where d is width and D is length, respectively). Therapeutic efficacy was evaluated by comparing the experimental group with control group.

- Results and Discussion

  - Polymer synthesis and characterization

The detailed synthesis route of PCBSA-SS-PCL-SS-PCBSA is shown in Scheme 2. PCL-diol introduced cystamine at the end groups [31]. After conjugation with CPADB, a PCL macro-RAFT agent was prepared and used for copolymerization with a CBMA monomer to obtain PCB-SS-PCL-SS-PCB. The 1HNMR spectra of the above intermediate products are shown in Fig.1s. Due to its reactive carboxylate anion, PCB has the advantage over other common zwitterionic polymers of being able to be further modified with amine-containing biomolecules via carbodiimide chemistry[32]. Here, we used benzene sulfonamide to modify PCB-SS-PCL-SS-PCB to PCBSA-SS-PCL-SS-PCBSA. Compared with PCB-SS-PCL-SS-PCB, the 1HNMR spectrum of PCBSA-SS-PCL-SS-PCBSA presents new characteristic peaks at o and p (Fig. 1A) corresponding to benzene sulfonamide [21], in addition to the peaks of PCL (at c, h, i and j) and the pendant group of PCB (at b, d, e and g). The modification rate was 92%, estimated by the integral area ratio of f and o. Finally, the molecular weight of PCBSA-SS-PCL-SS-PCBSA was calculated at 7200, and PCL and PCBSA weighed 2000 and 5200, respectively. FT-IR spectra confirmed that the modification was successful. As shown in Fig. 1B, the peak at 2958 cm−1 corresponds to the methylene in the repeated unit of PCL. The sharp peaks at 1726 cm−1 and 1151 cm−1 were attributed to the carbonyl and the vibration of C-N in the quaternary ammonium of PCB[33]. After the modification, both COO- stretching vibration around 1400 cm−1 and deformation vibration around 2700 cm−1 disappeared. The newly emerging peaks at around 1656 cm−1 correspond to the vibration of C=O in the tertiary amide[34]. The modification rate is adjustable by controlling the feed ratio of carboxylate and benzene sulfonamide. PCBSA-SS-PCL-SS-PCBSA with approximately 9% and 33% of modification was obtained and confirmed by 1HNMR spectra (Fig. 2s).

Scheme 2. Synthesis route of PCBSA-SS-PCL-SS-PCBSA. (i) CDI, anhydrous DCM, RT, 24 h; (ii) DMSO, pyridine, TEA, RT, 48 h; (iii) DCC, NHS, RT, 48 h; (iv) AIBN, THF, saturated salt water, 60 oC, 48 h; (v) EDC, NHS, RT, 24h.

Fig 1. 1HNMR (A) and FT-IR (B) spectrum of PCB-SS-PCL-SS-PCB and PCBSA-SS-PCL-SS-PCBSA.

  - Characterization of polymeric micelles

Polymeric micelles with PCL as a core and PCBSA as a shell (denoted as PCBSA micelles) were prepared by polymer self-assembly in aqueous solution. Hydrodynamic diameter distribution (Dh) was measured by DLS (Fig. 2A). The average diameter of the PCBSA micelles was approximately 91(5) nm with a narrow size distribution. TEM observation (Fig. 2B) showed a regular spherical morphology with a good dispersion. The mean diameter was approximately 70(2) nm. Protein resistance of PCB and PCBSA micelles was studied by size analysis after incubation in PB (pH 7.4) solution containing 50% FBS at 37oC. PCBSA micelles were slightly larger than PCB-SS-PCL-SS-PCB (PCB) micelles, indicating that the modification has little effect on self-assembling behavior in both these zwitterionic block copolymers. No obvious size increase was observed in either PCBSA or PCB micelles even after 72 h of incubation time (Fig. 1C).

Zwitterionic surfaces provide polymeric micelles with high antifouling capacity, thereby allowing their potential application as drug carriers in vivo.

To assess the surface charge changes of the polymeric micelles, their zeta potential was measured under different pH levels (from 7.6~5.8). As shown in Fig. 1C, PCBSA and PCB micelles had slightly negative charge at physiological pH (7.4~7.2) due to their zwitterionic surface. The surface potential of PCBSA micelles started to switch to positively charged below pH 7.0, with a sharp increase to 15mv zeta potential at pH 6.4. In contrast, PCB micelles remained negatively charged even at pH levels below 5.8. The charge reversal of PCBSA micelles suggests the polymer is pH-responsive. As the pKa of PCB is approximately 2.33 [35, 36], this polymer was inert within the pH range analyzed. After modification of the carboxylate group in PCB, the generated imine group was covalently bonded with the electron-withdrawing benzenesulfonyl and carbonyl groups, which can easily add or remove protons[37]. Under physiological pH (7.4~7.2), deprotonation of the imine group results in negative charge against zwitterionic quaternary ammonium. Protonated imine lost the charge at slightly acidic microenvironments, leading to an increase of the surface net charge. Micelles with 9% and 30% modification also showed similar charge changes, however, they had lower potential when compared to PCBSA micelles. Moreover, when these positively charged micelles were at physiological pH again, the surface potential returned to slightly negatively charged (Fig. 1E). Charge interconversion in PCBSA micelles are time independent and reversible due to the nature of the protonation/deprotonation reaction [21]. Positive micelles are able to recover their antifouling state upon ineffective internalization, which is critical to reduce adverse effects when they return to the bloodstream. As the PCBSA micelles have a disulfide bond between the shell and core, redox-responsiveness was also investigated (Fig. 1F). The micelles showed increased Dh and broadened PDI in a 10mM GSH solution for 4 h and 12 h. Micellar aggregation was likely caused by the cleavable disulfides and detached PCBSA shells.

Fig 2. Hydrodynamic diameter distribution f(Dh) (A) and TEM image (B) of PCBSA micelles; relationship of size and time of PCB and PCBSA micelles in PB (50 mM, pH 7.4) containing 50 % FBS (C); relationship between zeta potential of polymeric micelles and pH value (D). Charged interconversion of zeta potential as PCBSA micelles in different pH cycles (E); Hydrodynamic diameter distribution f(Dh) of PCBSA micelles in PB (50 mM, pH 7.4) containing 10 mM GSH (F). (standard deviation, n=3).

  - Characterization of DOX-loaded micelles

DOX was loaded into PCB and PCBSA micelles by using a coprecipitation approach. After lyophilizing and then dissolving the micelles in DMSO, drug-loading capacity was determined by UV-Vis spectrophotometry. DLC and DLE were 21% and 62%, respectively. The size of DOX-loaded PCBSA micelles measured by DLS was 122 nm, with a narrow PDI between 60-150nm (Fig.3A). TEM imaging reveals the micelles are well distributed and have a spherical shape with a diameter of approximately 96 nm (inserted in Fig.3A). A stable structure and uniform nanoscale size facilitate intracellular uptake and EPR effect in vivo[38]. In vitro drug-release profiles from DOX-loaded PCBSA micelles were conducted in the absence of GSH and in the presence of 10 M or 10 mM GSH at 37︒C, to mimic the physiological or intracellular microenvironment (Fig. 3B). A 36% decrease in DOX-release occurred at 10M GSH or without GSH within 24h. However, an accelerated release of DOX was observed at 10mM GSH, with approximately 67% DOX being released within 24h. Thus, the nanocarriers are stable in physiological conditions (low GSH concentration), while a rapid release of cargo is triggered in the tumor intracellular environment (high GSH concentration). This controlled drug-release behavior is due to the cleavage of disulfide bonds between shell and core, resulting in shell shedding and micelle aggregation. Indeed, drugs are rapidly extruded during the reassembly of deprotected micelles[39].

Fig.3 (A) Hydrodynamic diameter distribution f(Dh) and TEM image (inserted) of DOX-loaded PCBSA micelles. In vitro release profiles of DOX loaded PCBSA micelles in the absence or presence of 10Mm and 10 mM GSH.

  - In vitro cytotoxicity and cell uptake

in vitro cytotoxicity of empty and drug-loaded micelles was evaluated in HepG2 cells with MTT assays at pH 7.4 and pH 6.5. Both drug-free micelles exhibit high biocompatibility, even at 100 mg/L (Fig. 4A). Low cytotoxicity is derived from the biocompatible zwitterionic shell and PCL core. HepG2 cells were further incubated with free DOX, DOX-loaded PCB micelles, and DOX-loaded PCBSA micelles at pH 7.4 and pH 6.5 to assess viability (Fig.4B). IC50 (inhibitory concentration to produce 50% cell death) at pH 7.4 was 0.28 mg/L, 1.04 mg/L and 1.12, mg/L for the above conditions, respectively. The nanocarriers showed much lower cytotoxicity than free DOX, likely due to a reduction in cell uptake efficiency caused by the zwitterionic shell [40, 41]. However, at pH 6.5 DOX-loaded PCBSA micelles had an IC50 at 0.66 mg/L, which is higher than the IC50 of free DOX, but still lower than the IC50 of DOX-loaded PCBSA at pH 7.4 and DOX-loaded PCB micelles at pH 6.5 and 7.4. These results suggest that DOX-loaded PCBSA micelles have significantly higher cellular uptake in acidic conditions. As expected, PCBSA micelles were able to convert their zwitterionic surface charge at pH 7.4 into a positively charged surface at pH 6.5 (Fig. 2D), thereby promoting high affinity to cancer cells via electrostatic interactions with the negatively charged cell membrane. Fluorescence microscopy and flow cytometry confirmed these results (Fig. 4C). Indeed, fluorescent imaging reveals that DOX is present in HepG2 cells treated with DOX-loaded PCBSA and DOX-loaded PCB micelles at pH 7.4 and pH 6.5, indicating efficient drug release induced by intracellular GSH responsiveness. Interestingly, DOX-loaded PCBSA micelles showed stronger DOX fluorescence accumulation in HepG2 cells at pH 6.5 than at pH 7.4 and than DOX-loaded PCB micelles, which show similar DOX fluorescence intensity. Flow cytometry analyses (Fig. 4D) confirmed these results and further demonstrated that endocytosis of PCBSA micelles is pH-dependent.

Together these data show that DOX-loaded PCBSA micelles have excellent antifouling in physiological environments, active cell uptake in the tumor acidic microenvironment, and redox-responsive intracellular release. Thus, DOX-loaded PCBSA micelles are multifunctional nanocarriers with strong potential for in vivo clinical applications.

Fig.4. Toxicity of PCB and PCBSA micelles (A) and free DOX, DOX-loaded PCB micelles and DOX-loaded micelles in HepG2 cells (B) at pH 7.4 and 6.5, where the cells were incubated for 12h. Data are presented as the average (standard deviation (n=3); Fluorescence images (C) and flow cytometry analysis (D) in HepG2 cells, after treatment with DOX-loaded PCB micelles and DOX-loaded micelles at pH 7.4 and 6.5 for 4 h.

  - Blood Circulation and Biodistribution

The uniform nanosize and high stability in serum of DOX-loaded micelles should enhance their circulation time and accumulation efficiency at tumor sites. To test this, the pharmacokinetics and biodistribution of DOX-loaded micelles were further investigated in vivo. Free DOX, DOX-loaded PCB-micelles, and DOX-loaded PCBSA micelles were administrated intravenously into SD rats and then plasma DOX concentration was recorded at different time points. As shown in Fig. 5A, micelle loading significantly prolonged the circulation time of DOX. Specifically, approximately 12% of the injected dose was detected in the blood after 12 h with the micelles, whereas free DOX was eliminated within 2 h. Long circulation time can be attributed to the unique core-shell structure and zwitterionic surface of the micelles, and it can significantly increase the accumulation of the nanocarries at the tumor site via EPR effect[8]. The biodistribution of DOX in vital organs and tumors was assessed in nude mice bearing tumor models of human liver cancer injected with free DOX, DOX-loaded PCB micelles, or DOX-loaded PCBSA-micelles. Consistent with previous research [42], an increased accumulation of DOX in the tumor tissue and liver was detected in mice injected with DOX-loaded PCB micelles and DOX-loaded PCBSA-micelles, when compared to free DOX injection (Fig. 5B). These results suggest that these polymeric micelles have a similar in vivo distribution to that of small-size nanoparticles. In addition, DOX-loaded PCBSA micelles exhibited approximately 2-fold higher DOX accumulation at tumor sites than DOX-loaded PCB micelles. pH-dependent charge reversal of PCBSA micelles likely promotes internalization by tumor cells and reduces undesired elimination of the nanocarriers by high interstitial fluid pressure in the tumor microenvironment [43].

Fig. 5. DOX concentrations in blood plasma at different time points in SD rats and biodistribution of DOX in nude mice bearing tumor models of human liver cancer 12h after injection of free DOX, DOX-loaded PCB micelles and DOX-loaded PCBSA. Data are presented as the average (standard deviation, n=3).

  - In vivo antitumor efficiency

In vivo antitumor efficiency of DOX-loaded PCBSA was investigated in mice transplanted with tumor models of human liver cancer. When tumor size reached approximately 50 mm3, PBS, free DOX, DOX-loaded PCB micelles, or DOX loaded PCBSA micelles were injected through the tail vein. Tumor volume and body weight were measured and plotted as a function of time (Fig. 6A and B). As shown in Fig. 6A, tumor volume in mice treated with PBS increased rapidly. In contrast, tumor mice injected with free DOX, DOX-loaded PCB micelles, or DOX loaded PCBSA micelles exhibited slow tumor growth. Notably, DOX-loaded PCBSA micelles showed the strongest inhibition effect when compared to free DOX and DOX-loaded PCB micelles. Moreover, mice treated with either of the nanocarriers showed a slow increase in body weight with age (Fig. 6B), suggesting a relative low systemic toxicity when compared with free DOX. Indeed, mice injected with free DOX exhibited noticeable weight loss 8 days after injection. Tumor imaging and prolonged survival time (Fig. 6C and D) demonstrate that DOX-loaded PCBSA micelles improve DOX antitumor efficiency and reduce its adverse effects. A reduction in nonspecific interactions with normal organs and prolonged circulation time result from the excellent antifouling properties of these nanocarriers provided by the zwitterionic shells [44, 45]. Nanocarriers rapidly convert their zwitterionic surface into positive charges in response to the tumor acid microenvironment, thereby activating cellular uptake. After internalization of PCBSA micelles, reductive responsiveness accelerates the intracellular release of DOX, ultimately leading to effective inhibition of tumor growth with mild adverse effects in normal tissues.

Fig. 6. Tumor volume changes of tumor-bearing nude mice after treatment with PBS or free DOX, DOX-loaded PCB micelles and DOX-loaded PCBSA micelles at an equivalent daily dose of 4 mg/kg (A); Changes in mice body weight during the treatment (B); Photograph of excised solid tumors from each group on day 21 after treatment (C); Survival rates of mice after treatment (D). Data are presented as the average (standard deviation, n=3).

- Conclusions

We have successfully developed a polymeric micellar system with pHe and reductive dual responsiveness to tumor extracellular and intracellular biochemical features. With its acylsulfonamide-based betaine structure, the polyzwitterionic shell provided the polymeric micelles with highly sensitive, instant and reversible surface chemistry via deprotonation/protonation at tumor pHe. Moreover, the dual-response micellar carriers revealed better anticancer efficiency and reduced side effects in vitro and in vivo when compared to free drug or PCB micelles. Our results therefore show that one-step modification of conventional zwitterionic polymers such as PCB, is a simple and robust mechanism to selectively mediate nano-bio interactions between blood circulation and tumor sites. Thus, the development of intelligent NDDS via flexible design of zwitterionic nanoparticles is a feasible and valuable strategy with excellent potential for clinical applications in cancer bioimaging and treatment.